# Malaysian Journal of Analytical Sciences Vol 21 No 6 (2017): 1380 - 1388

# IN SITU HYDROGENATION OF LIQUID EPOXIDIZED NATURAL RUBBER USING DIIMIDE

# (Penghidrogenan In Situ Getah Asli Cecair Terepoksida Menggunakan Diimida)

# Nur Hanis Adila Azhar1, Hamizah Md Rasid1, Nur Aidasyakirah Mohd Tahir1, Siti Fairus M. Yusoff1, 2*

# 1School of Chemical Science and Food Technology, Faculty of Science and Technology

# 2Polymer Research Center (PORCE), Faculty of Science and Technology

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author:  sitifairus@ukm.edu.my

Received: 28 September 2016; Accepted: 6 March 2017

Abstract

# A low-molecular-weight liquid epoxidized natural rubber (LENR) was prepared through photosensitized degradation of epoxidized natural rubber with 50 mol percent of epoxy content (ENR-50). LENR was modified into hydrogenated liquid epoxidized natural rubber (HLENR) via in situ thermal degradation of arylsulfonyl hydrazide as a hydrogenating agent. The chemical structures of LENR and HLENR were characterized using Fourier transform infrared (FTIR) and 1H nuclear magnetic resonance (NMR) spectroscopies. The thermal behaviour of LENR and HLENR were analysed using thermogravimetric analysis (TGA). The molecular weight and polydispersity index (PDI) of LENR and HLENR were determined using gel permeation chromatography (GPC). The parameter studies on the hydrogenation of LENR were investigated based on the source of diimide, weight ratios of LENR: p-toluenesulfonyl hydrazide (TSH), temperature, reaction time and solvent of the reaction. The highest conversion of hydrogenation was achieved at 130 °C for 4 hours reaction time, with 1:1 weight ratio of LENR: TSH using o-xylene as a solvent.

# Keywords:  hydrogenation, liquid natural rubber, epoxidized, hydroxylated

# Abstrak

# Getah asli cecair terepoksida (LENR) dihasilkan melalui penguraian fotopemeka yang dijalankan ke atas getah asli terepoksida yang mempunyai 50 mol% kandungan epoksi (ENR-50). LENR dihidrogenkan kepada LENR terhidrogen (HLENR) melalui penguraian terma in situ dengan menggunakan agen penghidrogenan iaitu arilsulfonil hidrazida. Struktur kimia LENR dan HLENR dicirikan menggunakan spektroskopi inframerah transformasi Fourier (FTIR) dan resonans magnet nukleus (NMR). Sifat terma LENR dan HLENR dikaji menggunakan analisis termogravimetri (TGA). Berat molekul dan indeks kepoliserakan (PDI) dikaji menggunakan kromatografi penelapan gel (GPC). Kajian mengenai penghidrogenan LENR dikaji berdasarkan beberapa parameter tindak balas seperti sumber diimida, nisbah berat LENR: p-toluenasulfonil hidrazida (TSH), suhu, masa dan pelarut tindak balas. Penukaran penghidrogenan yang tertinggi diperolehi apabila tindak balas dijalankan pada suhu 130 °C selama 4 jam, dengan nisbah berat LENR:TSH sebanyak 1:1 serta menggunakan o-xilena sebagai pelarut.

# Kata kunci:  penghidrogenan, getah asli cecair, terepoksida, terhidroksil

References

- Wongthong, P., Nakason, C., Pan, Q., Rempel, G. L. and Kiatkamjornwong, S. (2013). Modification of deproteinized natural rubber via grafting polymerization with maleic anhydride. European Polymer Journal, 49(12): 4035 – 4046.

- Mooibroek, H. and Cornish, K. (2000). Alternative sources of natural rubber. Applied Microbiology and Biotechnology, 53(4): 355 – 365.

- Hayashi, Y. (2009). Production of natural rubber from Para rubber tree. Plant Biotechnology, 26(1): 67 –70.

- Kongparakul, S., Ng, F. T. T. and Rempel, G. L. (2011). Metathesis hydrogenation of natural rubber latex. Applied Catalysis A: General, 405(1-2): 129 – 136.

- Ayutthaya, W. D. N. and Poompradub, S. (2014). Thermal and mechanical properties of poly(lactic acid)/natural rubber blend using epoxidized natural rubber and poly(methyl methacrylate) as co-compatibilizers. Macromolecular Research, 22(7): 686 – 692.

- Pisuttisap, A., Hinchiranan, N., Rempel, G. L. and Prasassarakich, P. (2013). ABS modified with hydrogenated polystyrene-grafted-natural rubber. Journal of Applied Polymer Science, 129(1): 94 – 104.

- Nghia, P. T., Onoe, H., Yamamoto, Y. and Kawahara, S. (2008). Hydrogenation of natural rubber having epoxy group. Colloid and Polymer Science, 286(8-9): 993 – 998.

- Samran, J., Phinyocheep, P., Daniel, P., Derouet, D. and Buzaré, J. Y. (2004). Raman spectroscopic study of non-catalytic hydrogenation of unsaturated rubbers. Journal of Raman Spectroscopy, 35(12): 1073 –1080.

- Bhattacharjee, S., Bhowmick, A. K. and Avasthi, B. N. (1993). Hydrogenation of epoxidized natural rubber in the presence of palladium acetate catalyst. Polymer, 34(24): 5168 – 5173.

- Sanjoy Roy, S. and Bhattacharjee, B. R. G. (1993). Hydrogenation of epoxidized natural rubber. Journal of Applied Polymer Science, 49: 375 – 380.

- Ha, N. T., Shiobara, K., Yamamoto, Y., Fukuhara, L., Nghia, P. T. and Kawahara, S. (2015). Preparation and characterization of hydrogenated natural rubber with hydroxyl groups. Polymers for Advanced Technologies, 26(12): 1504 – 1511.

- Rasid, H. M., Azhar, N. H. A., Jamaluddin, N. and Yusoff, S. F. M. (2016). Mild approach for non-catalytic hydrogenation of liquid natural rubber using 2,4,6-trimethylbenzenesulfonyl hydrazide as the diimide source. Bulletin of the Korean Chemical Society, 37(6): 797 – 801.

- Mahittikul, A., Prasassarakich, P. and Rempel, G. L. (2007). Noncatalytic hydrogenation of natural rubber latex. Journal of Applied Polymer Science, 103(5): 2885 – 2895.

- Heijden, J. v. d. (2002). Natuurrubber 28 - 4th quarter 2002. Rubber-Stichting: pp 1 – 20.

- Rooshenass, P., Yahya, R. and Gan, S. N. (2016). Comparison of three different degradation methods to produce liquid epoxidized natural rubber. Rubber Chemistry and Technology, 89(1): 177 – 198.

- Hunig, S., Muller, H. R. and Thier, W. (1965). The chemistry of diamine. Angewandte Chemie International Edition, 4(4): 271 – 380.

- Wade, L. G. (2003). Organic chemistry (5th Edition). Prentice Hall, New Jersey.

- Abdullah, I. (1996). Process for manufacturing liquid natural rubber (LNR). Malaysian Patent, MY-108852-A.

- Jorge, R. M., Lopes, L., Benzi, M. R., Ferreira, M. T., Gomes, A. S. and Nunes, R. C. R. (2010). Thiol addition to epoxidized natural rubber: Effect on the tensile and thermal properties. International Journal of Polymeric Materials, 59(5): 330 – 341.

- Azhar, N. H. A., Jamaluddin, N., Md Rasid, H., Mohd Yusof, M. J. and Yusoff, S. F. M. (2015). Studies on hydrogenation of liquid natural rubber using diimide. International Journal of Polymer Science, 2015: 1–6.

- Mahmood, W. A. K. and Azarian, M. H. (2015). Thermal, surface, nanomechanical and electrical properties of epoxidized natural rubber (ENR-50)/ polyaniline composite films. Current Applied Physics, 15(5): 599 – 607.