Malaysian Journal of Analytical Sciences Vol 22 No 2 (2018): 203 - 218

RESPONSE SURFACE METHODOLOGY ON THE EFFECTS OF

SODA – ANTHRAQUINONE PULPING CONDITIONS ON OIL PALM

EMPTY FRUIT BUNCHES PULP PROPERTIES

(Kaedah Gerak Balas Permukaan Terhadap Kesan Faktor-Faktor Pemulpaan Soda-Antrakuinon Ke Atas Sifat-sifat Gentian Tandan Buah Kosong Kelapa Sawit)

Nurul Husna Mohd Hassan1*, Mazlan Ibrahim2, Nor Yuziah Mohd Yunus1

1School of Wood Industry, Faculty of Applied Sciences,

Universiti Teknologi MARA, Cawangan Pahang, Kampus Jengka, 26400 Bandar Tun Abdul Razak, Pahang

2School of Industrial Technology,

Universiti Sains Malaysia, 11800 USM Pulau Pinang, Malaysia

*Corresponding author: nurulhusna@uitm.edu.my

Received: 15 November 2016; Accepted: 29 January 2018

Abstract

Effects of soda–antrhraquinone (soda-AQ) pulping conditions on pulp properties of oil palm empty fruit bunches were studied by using response surface methodology (RSM) based on central composite design (CCD). Alkali charge (A), pulping temperature (T) and pulping time (t) were the pulping factors studied, with their ranges between 20 - 30%, 160 - 180 °C and 60 - 120 minutes, respectively. Pulp properties evaluated based on total yield (35.37 - 58.87%), screened yield (30.37 - 56.07%), Kappa number (6 – 16) and viscosity (5.43 - 16.02 cP). The effect of soda-AQ pulping conditions on oil palm empty fruit bunches fibers was clearly elucidated by the regression model obtained. The generated mathematical relationship showed that the optimum pulping condition was 27.30% alkali charge, temperature 160 oC at 60 minutes. This combination of mild pulping conditions level produced: total yield (55.54%), screened yield (53.20%), Kappa number (10) and viscosity (12.02 cP).

Keywords:  oil palm empty fruit bunches, pulp properties, response surface methodology

Abstrak

Kesan faktor-faktor pemulpaan soda-antrakuinon ke atas sifat-sifat gentian tandan buah kosong kelapa sawit telah dikaji dengan menggunakan kaedah gerak balas permukaan (RSM) berasaskan rekabentuk komposit berpusat (CCD). Julat faktor-faktor pemulpaan iaitu cas alkali (A), suhu pemulpaan (T) dan masa pemulpaan (t) adalah antara 20 – 30%, 160 – 180 oC dan 60 – 120 minit. Sifat-sifat gentian yang dinilai adalah berdasarkan jumlah keseluruhan (35.37 - 58.87%), hasil saringan (30.37 - 56.07%), nombor Kappa (6 – 16) dan kelikatan (5.43 - 16.02 cP). Pengaruh faktor-faktor pemulpaan soda-AQ ke atas gentian tandan buah kosong kelapa sawit dapat dijelaskan berdasarkan model regrasi yang diperolehi. Melalui persamaan matematik yang terhasil, pemulpaan optimum berlaku apabila faktor-faktor pemulpaan iaitu cas alkali, suhu pemulpaan dan masa pemulpaan diselaraskan pada 27.3%, 160 oC dan 60 minit. Penggunaan kombinasi aras faktor pemulpaan yang rendah ini dapat menghasilkan hasil keseluruhan (55.54%), hasil penskrinan (53.20%), nombor Kappa (10) dan kelikatan (12.02 cP).

Kata kunci:  tandan buah kosong kelapa sawit, sifat-sifat gentian, kaedah gerak balas permukaan

References

- Khozirah, S. and Khoo, K. C. (1991). Oil palm utilisation-review of research, Forest Research Institute (FRIM), Kepong, Selangor. Research Pamphlet No.107: 1-7

- Moll, H. A. J. (1987). The economics of oil palm. economics of crops in developing Countries No.2. Pudoc Wageningen, Netherlands.

- Sulaiman, O., Salim, N., Nordin, N.A., Hashim, R., Ibrahim, M. and Sato, M. (2012). The potential of oil palm trunk biomass as an alternative source for compressed wood. BioResearch, 7(2):688-706.

- Jalani, B. S. (2002). Prospects of elevating national oil palm productivity:  A Malaysian perspective. Oil Palm Industry Economic Journal, 2: 1–9.

- Abdullah, R. (2003). Short-term and long-term projection of Malaysian palm oil production. Oil Palm Industry Economic Journal, 3:32–36.

- MPOB (2015). Economic & industry development devision. oil palm planted area. Retrieved from: http://bepi.mpob.gov.my/index.php/statistics/area.html.

- Mohd-Fahmi, A., Othman, S., Rokiah, H. and Wan Noor Aidawati, W. N. (2015). An overview of the oil palm industry in Malaysia and its waste utilization through thermochemical conversion specifically via liquefaction. Renewable and Sustainable Energy Reviews, 50:1469-1484.

- Shafie, S., Mahlia, T., Masjuki, H. and Andriyana, A. (2011). Current energy usage and sustainable energy in Malaysia: A review. Renewable and Sustainable Energy Reviews, 15(9): 4370-4377.

- Wan Rosli, W. D., Leh, C. P., Zainuddin, Z. and Tanaka, R. (2003). Optimisation of soda pulping variables for preparation of dissolving pulps from oil palm fibre, Holzforschung, Walter de Gruyter, 57 (1), 106-113.

- MPOPC (2004). Malaysian palm oil promotion council, Kuala Lumpur, Malaysia. Retrieved from:http://www.mpopc.org.my.

- AIM (2013). National biomass strategy (2020): New wealth creation for Malaysia's biomass industry: Version 2.0, 2013. Agensi Inovasi Malaysia, Kuala Lumpur.

- Amiruddin, M. N., Abrahman, A. K. and Shariff, F. (2005). Market potential and challenges for the Malaysian palm  oil industry in  facing  competition from other vegetable oils. Oil Palm Industry Economic Journal, 5: 17–27.

- FAOSTAT (2015). Food and Agriculture Organization of the United Nations for a world without hunger. Retrieved from: http://faostat.fao.org/site/339/default. aspx.=

- Faizi, M. K., Shahriman, A.B, Abdul Majid, M. S., Shamsul, B. M. T., Ng, Y. G., Basah, S. N., Cheng, E. M., Afendi, M., Zuradzman, M. R., Khairunizam, W. A. N. and Hazry, D. (2017). An overview of the oil palm empty fruit bunch (OPEFB) potential as reinforcing fibre in polymer composite for energy absorption applications MATEC Web of Conferences 90: 01064.

- Eckert, R. C., Pfeiffer, G. O., Gupta, M. K. and Lower, C. R. (1984). Soda anthraquinone pulping of Douglas fir.  TAPPI: Journal of the Technical Association of the Pulp and Paper Industry, 67(11): 104-108.

- Hart, P. W and Rudie, A. W. (2014). Anthraquinone-A review of the rise and fall of a pulping catalyst. TAPPI: Journal of the Technical Association of the Pulp and Paper Industry, 13(10): 23-31.

- TAPPI test methods 1994 – 1995 (1994). T211 Ash in wood, pulp, paper and paperboard: combustion at 525°C. Vol. I, Atlanta, Georgia, Tappi Press.

- TAPPI test methods 1994 – 1995 (1994). T236 Kappa Number of Pulp. Vol. I, Atlanta, Georgia, Tappi Press.

- Browning, B. L. (1967). Methods of wood chemistry, Vol. II, Interscience Publishers, John Wiley & Sons, Inc.

- TAPPI test methods 1994 – 1995 (1994). T230 Viscosity of pulp (Capillary Viscometer Method). Vol. I, Atlanta, Georgia, Tappi Press.

- Kraber, S. (1997). Handbook for experimenters, Minneapolis: Stat-Ease Inc.

- Smook, G. A. (1992). Handbook for pulp & paper technologist, 2nd Edition, Vancouver, Angus Wilde Publications.

- Mimms, A., Kocurek, M. J., Pyatte, J. A. and Wright, E. E. (1989). Kraft Pulping: A compilation of notes, United State of America: Atlanta, Tappi Press.

- Khairunisak, A. R., Hong, O. B., Zakaria, S., Ahmad, S. and Mohd Yussof, M. N. (2002). Effect of Kraft pulping with anthraquinone and methanol on oil palm empty fruit bunches. Proceeding 5th national seminar on utilization of oil palm tree – oil palm biomass: opportunities and challenges in commercial exploitation, Kuala Lumpur, oil palm tree utilization committee of Malaysia: pp. 205-210.

- Iglesias, G., Bao, M., Lamas, J. and Vega, A. (1996). Soda pulping of Miscanthus sinensis. Effects of operational variables on pulp yield and lignin solubilization, Elsevier Science Ltd., Great Britain, Bioresource Technology, 58: 17-23.

- Casey, J. P. (1980). Pulp and paper: Chemistry and chemical technology, Vol. I, 3rd Edition, New York, John Wiley & Sons.

- Kleppe, P. J. (1970). Kraft pulping (feature review). TAPPI: Journal of the Technical Association of the Pulp and Paper Industry, 53(1): 35-47.