Malaysian Journal of Analytical Sciences Vol 23 No 2 (2019): 255 - 262

Synthesis and characterisation of nanohybrid anti-hypertensive drug, captopril intercalated into

zinc–Aluminium layered double hydroxide

# (Sintesis dan Pencirian Nanohibrid Ubat Anti-Hipertensi, Captopril Tersisip ke dalam

# Zink-Aluminium Hidroksida Berlapis Ganda)

# Zaemah Jubri1*, Siti Halimah Sarijo2, Monica Limau Anak Jadam1

# 1Centre for Advanced Materials,

# Universiti Tenaga Nasional, 43000 Kajang, Selangor, Malaysia

# 2Faculty of Applied Sciences,

# Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

# *Corresponding author:  zaemah@uniten.edu.my

Received: 19 August 2018; Accepted: 10 March 2019

Abstract

Captopril (CPL), an anti-hypertensive drug was intercalated into the interlayer spaces of zinc–aluminium layered double hydroxide (ZLDH) for the formation of zinc–aluminium–captopril (ZCPL) hybrid nanocomposite material by self-assembly method. The concentration of CPL used was 0.08 M with pH 7.5 in a constant 3:1 molar ratio of zinc (Zn) to aluminium (Al) in the mother liquor. As a result of the successful intercalation of CPL, powder X-ray diffraction pattern (PXRD) shows the basal spacing increased from 8.90 Å in ZLDH to 9.69 Å in the ZCPL nanohybrid material. Fourier transform infrared (FTIR) spectroscopy study shows the intercalated compound of ZCPL resembled the spectra of ZLDH and CPL, thus indicating the presence of both functional groups in ZCPL spectra. CHNS analysis shows the ZCPL nanohybrid material contains 30.63% (w/w) of CPL which was calculated based on the percentage of carbon in the sample. It was also found that the BET surface area increased from 1.7 m2/g in ZLDH to 10.9 m2/g in ZCPL. The pore texture of the resulting material was also changed as the result of the intercalation and the expansion of the basal spacing during the formation of the layered intercalated ZCPL nanohybrid material.

# Keywords:  captopril, anti-hypertensive drug, intercalation, layered double hydroxide, nanocomposite

# Abstrak

# Captopril (CPL) iaitu ubat anti-hipertensi telah berjaya disisipkan ke dalam ruang antara lapis hidroksida berlapis ganda bagi pembentukan bahan hibrid ZCPL nanokomposit melalui kaedah pembentukan sendiri. Kepekatan CPL yang digunakan adalah 0.08M dan pH 7.5 dengan nisbah kepekatan tetap Zn : Al adalah 3 : 1 dalam larutan akueous. Penyisipan anion captopril dapat ditentukan dari pengembangan jarak basal PXRD daripada 8.90 Å bagi zink-aluminium hidroksida berlapis ganda (ZLDH) kepada 9.69Å bagi bahan nanohibrid ZCPL. Analisis inframerah transformasi Fourier (FTIR) menunjukkan kehadiran gabungan kumpulan berfungsi bagi ZLDH dan CPL kelihatan pada spektra ZCPL. Ini membuktikan CPL telah berjaya disisipkan di antara ruang hidroksida berlapis ganda bagi pembentukan bahan nanokomposit tersebut. Analisis CHNS menunjukkan bahan nanohibrid ZCPL mengandungi CPL dengan peratusan 30.63 % (w/w) yang ditentukan melalui pengiraan peratusan karbon di dalam sampel nanohibrid ZCPL. Luas permukaan BET telah meningkat daripada 1.7 m2/g kepada 10.9 m2/g masing-masing bagi ZLDH dan ZCPL. Struktur liang bahan nanohibrid yang terhasil juga telah berubah disebabkan penyisipan captopril telah mengembangkan jarak basal, begitu juga dengan pembentukan liang yang lebih besar berlaku hasil dari pembentukan bahan nanohibrid, ZCPL.

Kata kunci:  captopril, ubat anti-hipertensi, sisipan, hidroksida berlapis ganda, nanokomposit

References

- Ladewig, K., Marcus, M., Zhi, P. X., Gray, P. P. and Gao, Q. (2010). Controlled preparation of layered double hydroxide nanoparticle and their application as gene delivery vehicles. Applied Clay Science, 48(12): 280 – 289.

- Suman, S., Sayantan, R., Rituparna, A., Tapan, K. C. and Jui, C. (2017). Magnesium, zinc and calcium aluminium layered double hydroxide drug nanohybrids: A comprehensive study. Applied Clay Science, 135: 493 – 509.

- Kuthati, Y., Kankala, R. K. and Lee, C. H. (2015). Layered double hydroxide nanoparticles or biomedical applications: Current status and recent prospects. Applied Clay Science, 112-113:100 – 116.

- Duan, X. and Evans, D. G. (2006). Layered double hydroxides, structure and bonding. Springer, Berlin, pp. 1 – 234.

- Sudipte, S., Ravi, T., Shiv, P., Shivali, D., Durga, P. M., Parimal, D., Shripathi, T., Mohan, K., Dipak, R. and Pralay, M. (2016). Layered double hydroxide as effective carrier for anticancer drug and tailoring of release rate through interlayer anions. Journal of Controlled Release, 224: 186 – 198.

- Salak, A. N., Tedim, J., Alena, I. Kuznetsova, Mikhail, L. Maria, G. S. F. (2010). Anion exchange in Zn-Al layered double hydroxide: In-situ X-ray diffraction study. Chemical Physics Letters, 495: 73 – 76.

- Chakrabarty, A. and Acharya, H. (2018). Facile synthesis of MgAl-layered double hydroxide supported metal organic framework nanocomposite for adsorptive removal of methyl orange dye. Colloid and Interface Science Communications, 24: 35 – 39.

- Lupa, L., Cocheci, L., Pode, R. and Hulka, L. (2018). Phenol adsorption using aliquat 336 functionalized Zn-Al layered double hydroxide. Separation and Purification Technology, 196: 82 – 95.

- Rives, V., Arco, M. D. and Martin, C. (2013). Layered double hydroxides as drug carriers and for controlled release of non-steroidal anti-inflammatory drugs (NSAIDs): A review. Journal of Controlled Release, 169: 28 – 39

- Zhang, K., Xu, Z. P., Lu, J., Tang, Z. Y., Zhao, H. J., Good, D. A. and Wei, M. Q. (2014). Potential for layered double hydroxides-based innovative drug delivery systems. International Journal of Molecular Sciences, 15: 7409 – 7428.

- Sipos, P. and Palinko, I. (2018). As-prepared and intercalated layered double hydroxides of the hydrocalumite type as efficient catalysts in various reactions. Catalysis Today, 306: 32 – 41.

- Zhang, S., Yan, Y., Wang, W., Gu, X., Li, H., Li, J. and Sun, J. (2018). Intercalation of phosphotungstic acid into layered double hydroxide by reconstruction method and its application in intumescent flame-retardant poly(lactic acid) composites. Polymer Degradation and Stability, 147:142-150.

- Sorrentino, A., Gorassi, M., Tortora, M., Vittoria, V., Constantino, U., Marmottini, F., Padella, F. (2005). Incorporation of Mg-Al hydrotalcite into a biodegradable poly(Ɛ-caprolactone) by high energy ball miling. Polymer 45: 1601 – 1608

- Dutta, K., Das, S. and Pramanik, A. (2012). Concomitant synthesis of highly crystalline Zn-Al layered double hydroxide and ZnO: Phase interconversion and enhanced photocatalytic activity. Journal of Colloid and Interface Science, 366: 28 – 36.

- Xiao, Y., Su, D., Wang, X., Wu, S., Zhou, L., Sun, Z., Wang, Z., Fang, S. and Li, F. (2017). Ultrahigh energy density and stable supercapacitor with 2D NiCoAl Layered double hydroxide. Electrochimica Acta, 253: 324 – 332.

- Shao, M., Zhang, R., Li, Z., Wei, M. Evans, D. E. and Duan, X. (2015). Layered double hydroxide toward electrochemical energy storage and conversion: Design, synthesis and applications. Chemical Communication, 51: 15880 – 15893.

- Gasser, M. S. (2009). Inorganic layered double hydroxides as ascorbic acid (vitamin C) delivery system –intercalation and their controlled release properties. Colloids Surface B, 73: 103 – 109

- Li, Y., Bao, W., Wu, H., Wang, J., Zhang, Y., Wan, Y., Cao, D. and Wang, Q. (2017). Delaminated layered double hydroxide delivers DNA molecules as sandwich nanostructure into cells via a non-endocytic pathway. Science Bulletin, 62(10): 686 – 692.

- Rojas, R., Linck, Y. G., Cuffini, S., Monti, G. and Giacomelli, C. E. (2015). Structural and physicochemical aspects of drugs release from layered double hydroxides and layered hydroxide salts. Applied Clay Science, 109-110: 119 – 126.

- Rives, V., Arco, M. and Martin, C. (2014). Intercalation of drugs in layered double hydroxides and their controlled release: A review. Applied Clay Science, 88-89: 239 – 269.

- Mohsin, S. M. N., Hussein, M. Z., Sarijo, S. H., Fakurazi, S., Arulselvan, P. and Yun Hin, T. Y. (2013). Synthesis of (cinnnamate-zinc layered hydroxide) intercalation compound for sunscreen application. Chemistry Central Journal, 26(7): 1 – 12.

- Legrouri A., Badreddine, A., Barroug, A., Roy, J. P., Besse, P. (1999). Influence of pH on the synthesis of Zn-Al-nitrate layered double hydroxide and the exchange of nitrate by phosphate ions. Journal of Material Science Letters, 18: 1077 – 1079.

- Hussein, M., Zainal, Z. and Hwa, T. K. (2000). Synthesis and properties of layered organic-inorganic hybrid material: Zn-Al layered double hydroxide-dioctyl sulfosuccinate nanocomposite. Journal of Nanoparticle Research, 2: 293 – 298.

- Srivastava, A., Khare, B., Argal, R. and Patel, S. (2003). Microdetermination of anti-hypertensive drug captopril using 2,6-dichlorophenol indophenol. Indian Journal of Chemistry, 42: 3036 – 3040.

- Jubri, Z., Mohd Yusuf, N. Z. A., Sarijo, S. H., Marsom, E. S. and Hussein, M. Z. (2017). Synthesis, characterization and controlled release properties of zinc-aluminium-beta-naphtoxyacetate nanocomposite. Journal of Porous Materials, 24(3): 573 – 582.

- Xu, Z. P. and Braterman, P. S. (2010). Synthesis, structure and morphology of organic layered double hydroxide (LDH) hybrids: Comparison between aliphatic anions and their oxygenated analogs. Applied Clay Science, 48: 235 – 242.