Malaysian Journal of Analytical Sciences Vol 24 No 2 (2020): 227 - 235

ELECTROBIOSYNTESIS OF NiO USING RAMBUTAN LEAVES FOR PHOTODEGRADATION OF REMAZOL BRILLIANT BLUE DYE

(Elektrobiosintesis NiO Menggunakan Ekstrak Daun Rambutan Untuk Fotodegradasi Pewarna Remazol Brilliant Biru)

Muhammad Farhan Hanafi, Noor Faizah Che Harun, Norzahir Sapawe*, Azizzami Raidin

Universiti Kuala Lumpur Branch Campus

Malaysian Institute of Chemical and Bioengineering Technology,

Lot 1988 Vendor City, Taboh Naning, 78000 Alor Gajah, Melaka, Malaysia

*Corresponding author:  norzahir@unikl.edu.my

Received: 28 April 2019; Accepted: 16 February 2020

Abstract

NiO catalyst was prepared through electrochemical method with rambutan (Nephelium lappaceum) leaves as an electrolyte. The effects of the preparation methods on the physical properties of the catalyst were studied via Fourier transform infrared spectroscopy (FTIR). The interaction between nickel species and bio-active compounds of rambutan leaves crude during the electrochemical was found to affect the NiO structure. An amount of 3.0 g L−1 of NiO was found to be the optimum dosage for 10 mg L−1 of Remazol Brilliant Blue (RBB) dye, which resulted in 83.7% of maximum degradation after 1 hour of contact time at pH 3 under fluorescent light. This study showed that the kinetics followed a pseudo-first order Langmuir–Hinshelwood model with the calculated values of Kr and KLH at 1.38 mg L−1 h−1 and 0.03 L mg−1, respectively. Measurements of the mineralization of RBB by COD and BOD5 analysis were 66.6% and 73.4%, respectively, before and after reaction. Therefore, the effectiveness of synthesized NiO by the electrobiosynthesis method was established and confirmed through this study. The synthesized NiO has a great potential as a photocatalyst in photocatalytic reaction for wastewater treatment.

Keywords:  electrobiosynthesis, nickel, remazol brilliant blue dye, degradation, light irradiation

Abstrak

Mangkin NiO disediakan melalui kaedah elektrokimia dengan ekstrak daun rambutan (Nephelium lappaceum) sebagai elektrolit. Kesan kaedah penyediaan ke atas sifat fizikal mangkin telah dikaji melalui spektroskopi inframerah transformasi Fourier (FTIR). Interaksi antara spesies nikel dan sebatian bio-aktif dari ekstrak daun rambutan semasa elektrokimia didapati mempengaruhi struktur NiO. Sejumlah 3.0 gL-1 NiO didapati sebagai dos optimum untuk 10 mgL-1 pewarna Remazol Brilliant Biru (RBB), yang menghasilkan 83.7% degradasi maksimum selepas 1 jam masa kontak di pH 3 di bawah lampu pendarfluor. Kajian ini juga menunjukkan bahawa kinetik mengikuti model Langmuir-Hinshelwood dengan pseudo pertama dengan nilai kiraan Kr dan KLH masing-masing adalah 1.38 mgL-1h-1 dan 0.03 Lmg-1. Pengukuran mineralisasi RBB oleh COD dan BOD5 adalah 66.6% dan 73.4%, sebelum dan selepas tindak balas. Oleh itu, keberkesanan sintesis NiO dengan kaedah elektrobiosintesis telah ditubuhkan dan disahkan melalui kajian ini. NiO yang disintesis mempunyai potensi besar sebagai fotokatalis dalam tindak balas fotokatalitik untuk rawatan air sisa.

Kata kunci:  elektrobiosintesis, nikel, pewarna remazol brilliant biru, degradasi, penyinaran cahaya

References

- Li, X. K., Ji, W. J., Zhao, J., Wang, S. J. and Au, C. T. (2005). Ammonia decomposition over Ru and Ni catalysts supported on fumed SiO2, MCM-41 and SBA-15. Journal of Catalysis, 236(2): 181-189.

- Singh, A., Kumar, V. and Srivastava, J. N. (2013). Assessment of bioremediation of oil and phenol contents in refinery wastewater via bacterial consortium. Journal Petroleum Environment Biotechnology, 4: 145-151.

- Sapawe, N., Jalil, A. A., Triwahyono, S., Sah, R. N. R. A., Jusoh, N. W. C. and Hairom, N. H. H. (2013). Electrochemical strategy for grown ZnO nanoparticles deposited onto HY zeolite with enhanced photodecolorization of methylene blue: Effect of the formation of Si-O-Zn bonds. Applied Catalysis A: General, 456: 144-158.

- Sapawe, N., Jalil, A. A. and Triwahyono, S. (2013). One-pot electro-synthesis of ZrO2-ZnO/HY nanocomposite for photocatalytic decolorization of various dye-contaminants. Chemical Engineering Journal, 225: 254-265.

- Venu, G. D. and Sahle, E. E. (2008). Catalytic oxidation of dimethyl sulfide with ozone: effects of promoter and physico-chemical properties of metal oxide catalysts. Applied Catalyst A: General, 348(1): 86-93.

- Bokare, A. D., Chikate, R. C., Rode, C. V. and Paknikar, K. M.  (2008). Iron-nickel bimetallic nanopartilcles for reductive degradation of azo dye Orange G in aqueous solution. Applied Catalysis B: Environmental, 79: 270-278.

- Petya, K., Naydenov, A., Christoskova, S. and Mehandjiev, D. (2006). Alumina-supported nickel oxide for ozone decomposition and catalytic ozonation of CO and VOCs. Journal of Chemical & Engineering, 122: 41-46.

- Xinyu, Z., Li, X. and Qin, W. (2009). Investigation of the catalytic activity for ozonation on the surface of NiO nanoparticles. Chemical Physics Letter, 479(4): 310-315.

- Swami, A., Selvakannan, P. R., Pasricha, R. and Sastry, M. (2004). One-step synthesis of ordered two-dimensional assemblies of silver nanoparticles by the spontaneous reduction of silver ions by pentadecylphenol Langmuir monolayers. The Journal of Physical Chemistry B, 108: 19269-19275.

- Sapawe, N., Jalil, A. A., Triwahyono, S., Adam, S. H., Jaafar, N. F. and Satar, M. A. H. (2012). Isomorphous substitution of Zr in the framework of aluminosilicate HY by an electrochemical method: Evaluation by methylene blue degradation. Applied Catalysis B: Environmental, 125: 311-323.

- Sapawe, N., Rustam, M. A., Mahadzir, M. H. H., Lani, M. K. E. M., Raidin, A. and Hanafi, M. F. (2019). A novel approach of in-situ electrobiosynthesis of metal oxide nanoparticles using crude plant extract as main medium for supporting electrolyte. Materials Today: Proceedings, 19(4): 1441-1445.

- Hanafi, M. F., Sapawe, N., Rahim, M. Z. A., Rahman, N. N., Rahman, A. H. A. and Ahmad, A. A. (2016). Performance of EGZrO2-EGFe2O3/HY as photocatalyst and its efficacy in decolorization of dye-contaminants. Malaysian Journal of Analytical Sciences, 20(5), 1052-1058.

- Hanafi, M. F. and Sapawe, N. (2018). Remarkable degradation of methyl orange by tetragonal zirconia catalyst. Materials Today: Proceedings, 5(10), 21849-21852.

- Hanafi, M.F. and Sapawe, N. (2019). The potential of ZrO2 catalyst toward degradation of dyes and phenolic compound. Materials Today: Proceedings, 19(4): 1524-1528.

- Hanafi, M. F. and Sapawe, N. (2019). Electrosynthesis of ZrO2 nanoparticles with enhanced removal of phenolic compound. Materials Today: Proceedings, 19(4): 1529-1532.

- Hanafi, M. F. and Sapawe, N. (2019). Effect of calcination temperature on the structure and catalytic performance of ZrO2 catalyst in phenol degradation. Materials Today: Proceedings, 19(4): 1533-1536.

- Hanafi, M. F. and Sapawe, N. (2019). Electrogenerated zirconia (EGZrO2) nanoparticles as recyclable catalyst for effective photocatalytic degradation of phenol. Materials Today: Proceedings, 19(4): 1537-1540.

- Sapawe, N. and Hanafi, M. F. (2015). Facile one-pot electrosynthesis of high photoreactive hexacoordinated Si with Zr and Zn catalyst. RSC Advances, 5(92): 75141-75144.

- Sapawe, N. (2015). Hybridization of zirconia, zinc and iron supported on HY zeolite as a solar-based catalyst for the rapid decolorization of various dyes. New Journal of Chemistry, 39(6): 4526-4533.

- Sapawe, N. (2015). Effective solar-based iron oxide supported HY zeolite catalyst for the decolorization of organic and simulated dyes. New Journal of Chemistry, 39(8): 6377-6387.

- Rahdar, A., Aliahmad, M. and Azizi, Y. (2015). NiO nanoparticles: Synthesis and characterization. Journal of Nanostructures, 15: 145-151.

- Yuvakumar, R., Suresh, J., Joseph, A. N., Sundrarajan, M. and Hong, S. I. (2014). Rambutan (Nephelium lappaceum L.) peel extract assisted biomimetic synthesis of nickel oxide nanocrystals. Material Letters, 128(1): 170-174.

- Algubili, A. M., Alrobayi, E. M. and Alkaim, A. F. (2015). Photocatalytic degradation of remazol brilliant blue dye by ZnO/UV process. International Journal Chemistry and Science, 13(2): 911-921.

- Das, D. P., Baliarsingh, N. and Parida, K.M. (2007). Photocatalytic decolorisation of methylene blue (MB) over titania pillared zirconium phosphate (ZrP) and titanium phosphate (TiP) under solar radiation.  Journal of Molecular Catalysis A: Chemical, 261: 254-261.

- Sapawe, N., Jalil, A. A., Triwahyono, S., Adam, S. H., Jaafar, N. F. and Satar, M. A. H. (2012). Isomorphous substitution of Zr in the framework of aluminosilicate HY by an electrochemical method: Evaluation by methylene blue degradation. Applied Catalysis B: Environmental, 125: 311-323.